Section 02910     STALITE  PLANTING MEDIA FOR ATRIUM PLANTERS

### PART 1 – GENERAL

- SUMMARY

- Section Includes:

  - Planting Media

- Related Sections

  - REFERENCES

- ASTM – American Society for Testing and Materials

- USDA – US Department of Agriculture

  - DEFINITIONS

1.03 SYSTEM DESCRIPTION

# A.  Planting Media premixed containing the four components below:

40% CA9 Stalite

# 20%  USGA Rootzone Sand

# 20% Compost

# 20% Aged Pine Bark Fines

1.04  SUBMITTALS

  - QUALITY ASSURANCE

  - WORK CONDITIONS

  - SEQUENCING AND SCHEDULING

PART 2 – PRODUCTS

2.02  MATERIALS

A.   Stalite #9

Sieve Size        	% Retained

#4	         	 0-15%

#8                   	60-80%

#16                 	85-90%

#30		 90-95%

#100		 95-98%

#200		 95-100%

B.	USGA Root Zone Sand

1.  Grain Size Distribution (ASTM C136-95A)

Sieve Size             % Retained on Sieve

2.00 mm                   <3%

1-2 mm                     10% max

0.5 -1 mm                 45% max

.25 -.5 mm                 35% - 75%

.15 -.25 mm               15% max

.05 - .15 mm 		  5% max

- Compost

Minus 1/2” screen

- Aged Pine Bark Fines

Minus ½”  screen.