- Stalite Planting Applications For Sodding Compacted Soils

2.1 Product

A.        STALITE  PermaTill Rotary Kiln Expanded Slate

1.  ASTM C29 Unit Dry Weight loose (52 lb./cf to 55 lb./cf)

2. ASTM C127 Specific Gravity to meet 1.45 to 1.60, SSD

5/16” STALITE  PermaTill Expanded Slate

3/8” - #8 (5/16”) PermaTill Expanded Aggregate

Sieve Size        % Passing

½”                               100

3/8”                      80 - 100

#4                          5 - 40

#8                            0 - 20

#16                          0 - 10

2.2 Tilling Stalite Into Existing Soil

- Using a mechanical tiller.

  - Kill any undesirable vegetation with approved herbicide.

  - Remove dead vegetation and other debris.

  - Subsoil, disk or till soil to a depth of 8” to 12”

  - For a 50% amendment:  place 4 inches of Stalite over the entire area to be sodded.

  - If organic matter is required, add 1” to 2” of an approved compost over the surface area to be planted.

  - Using a tiller, completely till the four application of Stalite (with compost) a minimum of eight inches deep into the soil.

  - Rake the surface smooth and install sand based sod as specified.